HISTORIC SAMPLING REPORT — DOCUMENT 03.1  |  DATA ROOM

Historic Sampling

Jingo Gold Project — Compiled Historic Production & Sampling Records

# Overview

This document compiles the available historic production and modern sampling records for the Jingo Gold Project. All data is reproduced from original source documents and is provided as a reference for due diligence. Original source records (Boise Assayer & Metallurgy assay certificates and the Jingo Gold — Project Summary) are available in this section of the data room (Document 03.2).

Important: All sampling pre-dates current NI 43-101 (Canadian) and SK 1300 (U.S. SEC) QA/QC standards. Sample numbers, descriptions, and assay values are reproduced from the original 1985–86 assay certificates. Independent verification by twin sampling under modern QA/QC protocols is recommended before any reliance on the results.

# 1933 Production Record

The most significant historic production record for the Jingo property is a documented shipment of 153 tons of ore in 1933, with the following grade:

| Year | 1933 |
| --- | --- |
| Tonnage Shipped | 153 tons |
| Gold Grade | 1.28 oz/t Au (≈ 39.8 g/t Au) |
| Silver Grade | 6.70 oz/t Ag (≈ 208 g/t Ag) |
| Gold Content | ≈ 196 oz Au |
| Silver Content | ≈ 1,025 oz Ag |
| Classification | Very strong shipping-grade material |
| Source | Historic district records |

Earlier records (circa 1903) note average gold values of $15–$25 per ton at then-prevailing gold prices, indicating continuous production from the system between approximately 1893 (discovery) and the early 1930s.

# August 1985 Sampling Program

Boise Assayer & Metallurgy report dated August 14, 1985. Seven samples submitted, primarily targeting the historic ore dumps and vein discovery zone.

| Sample | Lab No. | Description | Au oz/t | Ag oz/t |
| --- | --- | --- | --- | --- |
| 2801 | 20418 | Jingo dump — composite | 0.171 | 0.92 |
| 2802 | 20419 | Jingo dump — composite | 0.107 | 0.94 |
| 2803 | 20420 | Jingo dump — composite | 0.133 | 0.76 |
| 2804 | 20421 | Jingo vein sample at top just below discovery point, from back-hoe cut, south side | 0.026 | 0.26 |
| 2805 | 20422 | Jingo vein sample at top just below discovery point, from back-hoe cut, north side | 0.168 | 1.25 |
| 2806 | 20423 | Outcrop at east end of the Jingo claim | 0.072 | 0.34 |
| 2807 | 20424 | Outcrop at west end of the Hornet claim | 0.089 | 0.11 |
| AVG | — | Average of 7 samples | 0.109 | 0.65 |

# October 1985 Sampling Program

Boise Assayer & Metallurgy report dated October 15, 1985. Thirteen samples (including one check assay) targeting specific vein textures and alteration phases. This program identified the highest-grade modern result on record: sample 6803 returning 1.057 oz/t Au and 11.25 oz/t Ag from bug-hole quartz.

| Sample | Lab No. | Description | Au oz/t | Ag oz/t |
| --- | --- | --- | --- | --- |
| 6801 | 22666 | Rose quartz — Fe stain with blood-red stains | 0.322 | 5.33 |
| 6802 | 22667 | White quartz with green and some Fe stain | 0.009 | 0.22 |
| 6803 | 22668 | Bug hole quartz / spider web of Fe stain + orange ★ PEAK | 1.057 | 11.25 |
| 6804 | 22669 | Gouge contact at footwall, mostly green | 0.131 | 0.28 |
| 6805 | 22670 | Blue-green quartz with yellow-red-Fe stains | 0.017 | 0.39 |
| 6806 | 22671 | Blue-green quartz with white quartz stringers, large pieces white quartz | 0.014 | 0.22 |
| 6807 | 22672 | Granite-looking — green-gray-black & Fe stain, decomposed altered pyrite & Cu stain | 0.025 | ND |
| 6808 | 22673 | Gray-green quartz with large pyrite & Fe stains | 0.034 | 0.94 |
| 6809 | 22674 | Blue-green granular quartz with brown spots & black leaf pattern, some bug hole exterior | 0.004 | 0.56 |
| 6810 | 22675 | Fine-grain quartz with Cu stains & small pyrite | 0.299 | 2.86 |
| 6811 | 22676 | White to light gray quartz with Fe spider web throughout, opalised to calcitic | 0.734 | 8.18 |
| 6811-C | 22676 | Check assay of sample 6811 | 0.720 | 8.84 |

# May 1986 Sampling Program

Twelve samples collected in May 1986, with detailed descriptions of channel cut widths and structural setting. This program yielded the highest reported true-width channel sample (sample 877: 8 feet of quartz vein at 0.532 oz/t Au) and another high-grade grab (sample 878: 0.802 oz/t Au).

| Sample | Description | Au oz/t | Ag oz/t |
| --- | --- | --- | --- |
| 872 | Random chip sample of bull quartz outcrop, 100' × 10', north-end center of Hornet claims | 0.013 | ND |
| 873 | Cut 10' of granite with quartz seam exposed on north side prospect pit; little FeOx | 0.011 | ND |
| 874 | Cut 12.5' of cross quartz structure in front of prospect pit; HW & FW not exposed | 0.013 | ND |
| 875 | Cut 4' of quartz with 1' intrusive on HW in prospect pit; 0.1' FeOx zone in quartz, FW not exposed | 0.015 | ND |
| 876 | Cut 9.5' SiO2 granite with FeOx-boxwork; sample only HW country rock; major shear gouge | 0.010 | 0.36 |
| 877 | Cut 8' qtz vein, SiO2 granite with 1' gouge — country rock from face caved adit above dump ★ | 0.532 | 0.27 |
| 878 | Grab — high-grade; FeOx-staining rock from main dump ★ | 0.802 | 1.95 |
| 879 | Grab — dump sample from area of #872 | 0.011 | 0.07 |
| 880 | Grab — dump sample from area of #873 | 0.014 | ND |
| 881 | Grab — dump sample from area of #874 | 0.007 | 0.22 |
| 882 | Grab — dump sample from area of #875 | 0.008 | 0.08 |
| 883 | Grab — dump sample from area of #876 | 0.010 | 0.19 |

# Summary of Highest-Grade Modern Samples

| Sample 6803 (Oct 1985) | 1.057 oz/t Au, 11.25 oz/t Ag — peak modern result, bug hole quartz |
| --- | --- |
| Sample 878 (May 1986) | 0.802 oz/t Au, 1.95 oz/t Ag — high-grade FeOx-stained dump grab |
| Sample 6811 (Oct 1985) | 0.734 oz/t Au, 8.18 oz/t Ag — white-gray quartz, Fe spider web |
| Sample 877 (May 1986) | 0.532 oz/t Au, 0.27 oz/t Ag — 8' true-width channel cut in vein |
| Sample 6801 (Oct 1985) | 0.322 oz/t Au, 5.33 oz/t Ag — rose quartz with blood-red Fe stains |
| Sample 6810 (Oct 1985) | 0.299 oz/t Au, 2.86 oz/t Ag — fine-grain qtz with Cu stains |

# Key Observations

- The peak grades are consistently associated with a specific quartz texture — "bug hole" quartz with spider-web Fe staining — providing a clear visual targeting criterion for future sampling and core logging.

- The 8-foot channel cut at 0.532 oz/t Au (sample 877) is the only true-width sample of the main vein available in the records. This is a particularly important data point because it represents a fair-width grade, not a high-grading grab.

- The check assay on sample 6811 (0.720 oz/t Au vs original 0.734 oz/t Au) shows good repeatability and supports the validity of the high-grade reports.

- Silver values track gold values with a typical Ag:Au ratio of approximately 5–10:1 in the higher-grade samples — consistent with epithermal vein systems.

- Sampling on the Hornet claims at the north end of the property returned lower but consistently anomalous gold values (samples 872–874 at 0.011–0.015 oz/t Au), confirming along-strike continuity of the system.

DISCLAIMER

All sampling data reproduced in this document is from historic sources (1933 production record; Boise Assayer & Metallurgy reports of 1985–86) and pre-dates modern NI 43-101 and SK 1300 QA/QC standards. Sample chain-of-custody, lab certification, and assay quality control records may be incomplete. Modern twin sampling and verification under appropriate QA/QC protocols is required before any reliance on these results for resource estimation or transaction valuation.